## Slide 1: LSI design training with SKY130
Analog LSI design Part 1
Mizuki Mori , https://github.com/3zki
Last update: 2024/12/31

## Slide 2: Log
2024/12/31 Initial release of English version

## Slide 3: Lab data
Development Environment Setup Script (Windows WSL + Ubuntu 22)
  https://github.com/3zki/wsl_osic
Analog LSI design Part 1
  https://github.com/3zki/lab240921
Please download these materials by “ git clone “ etc…

## Slide 4: Analog LSI design Part 1
Make a CMOS inverter (NOT logic gate)
  Background knowledge
  Schematic design
  Layout design
  Post layout simulation (Parasitic extraction)

## Slide 5: Background knowledge of LSI
Planar FET structure

## Slide 6: What is LSI?
There are various types of LSIs. Design methods and characteristics differ among them.
SKY130 and GF180MCU are planar MOSFET process ☞ We can make Pch MOSFET and Nch MOSFET
The manufacturing limit for planar FET is about 28 nm. High-density logic circuits such as CPU use completely different process such as FinFET and GAA-FET.
Planar 130nm is obsoleted for logic circuits, but cheaper than the FinFET and still be used for analog LSI.
https://commons.wikimedia.org/wiki/File:Multigate_models.png
https://commons.wikimedia.org/wiki/File:MOS-FET_gate_model_(n-channel)_E.PNG
Planar FET (~28nm)
FinFET (25nm ~ 7nm)

## Slide 7: What can we make with the planar FET process?
Planar MOSFET: PMOS, NMOS
  SKY130 supports 1.8V, 3.3V 5.0V, 10.5V, 16V, 20V devices
Diode
Resistor: Polysilicon resistor, Active Resistor (Diffusion Resistor), Nwell Resistor
Capacitor: MOS capacitor, Diffusion Capacitor, MIMCAP*, MOMCAP(Metal-Oxide-Metal)
Varactor diode(Varicap)*
Lateral bipolar transistor*: PNP, NPN
* = Not supported for some processes. SKY130 supports them.

## Slide 8: What is the MOSFET?
Similar to a potentiometer.
  Turning the knob changes the resistance from ≒ 0Ω.
  Main characteristics are taper and maximum resistance value.
  Taper: relation between the angle of knob and the resistance. (For example: log, linear, inverse-log)

## Slide 9: What is the MOSFET?
In MOSFET, the characteristics are based on current. (Basically, we never think in terms of resistance.)
Difference from potentiometer
  Turning the Gate voltage changes the current between Drain and Source from ≒ 0A (≒∞Ω)
  Main characteristics are current curves (Drain-Source current
    Minimum resistance is calculated from the current curve (on-resistance ）
  Characteristics of current variation is process-dependent (Threshold voltage , Transconductance )

## Slide 10: What is the MOSFET?
Equivalent circuit representing a MOSFET as a passive element
The variable resistor between drain and source should be a current source. (but it is also inaccurate though.)
The main characteristic of MOSFETs is transconductance.
Another main characteristic is saturation which acts as a current source in a specific Drain-Source voltage () region.
Gate capacitance also exists between gate-drain and gate-body, but only gate-source is drawn due to visual issues.

## Slide 11: Potentiometer vs. nMOS
（GΩ）
（μA）
（V）
（V）
Hard to see if the vertical axis is in Ω
Engineers are interested in this section.

## Slide 12: Characteristics of nMOS
（μA）
（V）
Threshold Voltage Threshold gate-source voltage at which current begins to conduct
Transconductance Gate-source voltage variation vs. drain-source current variation
on-resistance Drain-source resistance in on-state

## Slide 13: Design flow of Analog LSI
How to design Analog LSI

## Slide 14: Design flow of Analog LSI
Draw schematics and test benches
Simulation
Draw layouts based on schematics
Layout verification
Post-layout simulation: Simulation with parasitic components
（Place on frame）

## Slide 15: Draw the schematics and test benches

## Slide 16: Simulate

## Slide 17: Draw the layouts

## Slide 18: Extract parasitic components

## Slide 19: Make test benches again

## Slide 20: Simulate with parasitic components (Post-layout simulation)
149.9ps
15.0ps
164.9ps
Parasitic capacitance worsens responsiveness
After
Before

## Slide 21: Background knowledge of LSI
Know the characteristics of the process

## Slide 22: Before designing...
We want to know the characteristics of CMOS!
  Vgs – Ids curve
  Operational Point analysis
  Vds – Ids curve

## Slide 23: Vgs – Ids curve / on-resistance measurement
Simulate the on-resistance of CMOS (L=0.15μm, W=1.0μm, Vds=1.8V)
1. Place voltage sources vp (V=1.8) and vn (V=1.8) between drain and source 2. Place voltage source vg(V=0) between gate and GND 3. Sweep the voltage of vg between 0V and 1.8V by DC analysis 4. Find current consumption of voltage sources vp and vn
Format of DC anaylsis dc [voltage source] [start voltage] [end voltage] [step width]
Current consumption of voltage sources ngspice: vp#branch, vn#branch or gaw(waveform viewer): i(vp), i(vn)

## Slide 24: Example of test bench (L=0.15μm)
GND is zero (0) in the SPICE netlist
Be sure to include GND or 0 as a reference.
“VSS” is not converted to 0
vgsbench.sch

## Slide 25: Simulation results
> plot vp#branch vn#branch

## Slide 26: Output data
wrdata command saves specific data *) hoge#branch -> current consumption of voltage source hoge
vp.txt
0.00000000e+00 -2.00726126e-04
1.00000000e-01 -1.76783868e-04
2.00000000e-01 -1.52856174e-04
3.00000000e-01 -1.29370810e-04
4.00000000e-01 -1.06779404e-04
5.00000000e-01 -8.55349063e-05
6.00000000e-01 -6.60656564e-05
7.00000000e-01 -4.87492484e-05
8.00000000e-01 -3.38904626e-05
9.00000000e-01 -2.17083481e-05
1.00000000e+00 -1.23365952e-05 1.10000000e+00 -5.82743752e-06 1.20000000e+00 -2.07958988e-06 1.30000000e+00 -5.36969830e-07 1.40000000e+00 -1.19564554e-07 1.50000000e+00 -2.81003906e-08 1.60000000e+00 -6.92577344e-09 1.70000000e+00 -1.63614705e-09 1.80000000e+00 -3.19909099e-10
vn.txt
0.00000000e+00 -2.03659312e-12 1.00000000e-01 -4.80682161e-12 2.00000000e-01 -3.99689171e-11 3.00000000e-01 -4.84302376e-10 4.00000000e-01 -5.99945693e-09 5.00000000e-01 -7.04327370e-08 6.00000000e-01 -6.97912479e-07 7.00000000e-01 -4.74592920e-06 8.00000000e-01 -1.91451559e-05 9.00000000e-01 -4.83465908e-05 1.00000000e+00 -8.87674453e-05 1.10000000e+00 -1.35141610e-04 1.20000000e+00 -1.84593052e-04 1.30000000e+00 -2.35816015e-04 1.40000000e+00 -2.88115929e-04 1.50000000e+00 -3.41048569e-04 1.60000000e+00 -3.94303222e-04 1.70000000e+00 -4.47655558e-04 1.80000000e+00 -5.00941446e-04

## Slide 27: On-resistance
Characteristics of on-state at L=0.15μm, W=1.0μm
PMOS: 0.00000000e+00 -2.00726126e-04 Vds = 1.8V → 1.8/2.01e-4 = 9.0kΩ NMOS: 1.80000000e+00 -5.00941446e-04 Vds = 1.8V → 1.8/5.01e-4 = 3.6kΩ On-resistance and W are roughly inversely related → aligned at We usually change W instead of L.

## Slide 28: Operational Point analysis（OP）
op command calculates parameters such as vth and gm.
Specify the proper voltage conditions.
  gm, vdsat etc... are voltage dependent.
gm is useful for calculating currents by hand.
Off-state
On-state
opbench.sch

## Slide 29: Note: transconductance gm
Have you ever seen these formulas before?
in linear region ()
in saturation region ()
gm is a derivative parameter of the above equation, that is,
in linear region ()
in saturation region ()
→ in saturation region

## Slide 30: ngspice command: show m
The results can be saved to plain text.
  show m > ~/test.txt

## Slide 31: Parameter of transistor
Basically, we change (set) W and L
  W ：Channel width
  L ：Channel length *) Actual channel length is a bit short
The overlapped area of the polysilicon gate and diffusion is the “transistor” When sufficient potential is given to the gate, a channel is formed.
m, nf, mf, etc... specify the number of multi-finger gate. (Described later in the layout description)
Almost Channel
Drain
Source
Gate

## Slide 32: nMOS diagram
D
G
n+
p
n+
S
B

## Slide 33: nMOS diagram
n
D
n+
n
p
n
n+
no current yet
Since Vd > Vs,
the depletion layer on the drain side is larger than the depletion layer on the source side
Hole on substrate moves to gate at Vg > 0
→formation of deplation layer
G > 0V
S = 0V
B = 0V

## Slide 34: nMOS diagram
D
G >> 0V
S = 0V
n
B = 0V
p
have a current
n+
n+
Inversion layer is easily formed when the depletion layer is thin and difficult to form when it is thick
Conduction electrons become majority carriers at Vg >> 0
→Formation of inversion layer (Vth)

## Slide 35: nMOS diagram
D
G >> 0V
S = 0V
n
B = 0V
p
have a current
Inversion layer is easily formed when the depletion layer is thin and difficult to form when it is thick
Conduction electrons become majority carriers at Vg >> 0
→Formation of inversion layer (Vth)
Effective channel length
Channel length
n+
n+

## Slide 36: What happens if channel width W is changed?
A larger channel width results in a wider current path, which increases the drain-source current.
For transistors with the same channel length, the channel width is proportional to the drain-source current.
W
W
2W
＝

## Slide 37: What happens if channel length L is changed?
The effect of the short channel effect completely changes the characteristics. Basically, Ids increases as channel length L decreases, but short-channel effects also occur...
DIBL (Drain Induced Barrier Lowering) decreases Vth for an increase in Vds.
Increasing subthreshold swing increases punch-through in subthreshold region
  Leakage current increases in the off state, and Ids variation relative to Vgs variation becomes smaller (slower) → Switching characteristics deteriorate
Channel length modulation effect increases Ids variation relative to Vds variation and does not saturate (The current is not constant on the Vds - Ids curve.)

## Slide 38: Vds – Ids curve
Get the Vds - Ids curve of NMOS and see the effect of channel length modulation effect
Under construction!

## Slide 39: Demonstration of Analog LSI design
Make a CMOS inverter

## Slide 40: Design flow of Analog LSI
Draw schematics and test benches
Simulation
Draw layouts based on schematics
Layout verification
Post-layout simulation: Simulation with parasitic components
（Place on frame）

## Slide 41: Design of CMOS inverter
Topology verification
What is the performance of CMOS inverter?
Elmore delay model
  Input / Output conditions
Delay time simulation
meas command
Model corner simulation

## Slide 42: CMOS inverter, NOT logic gate
Input A | Output Q
L | H
H | L
Input A | Output Q
Vss | Vdd
Vdd | Vss
https://commons.wikimedia.org/wiki/File:CMOS_Inverter.svg

## Slide 43: Logic verification（Topology verification)
In a CMOS inverter, the output should be inverted with the input
  Input = 0 V → Output = Vdd V, Input = Vdd V → Output = 0 V
  See how a CMOS inverter works with DC analysis
DC analysis Steady-state response when voltage is varied
tran analysis Transient response when time is varied
AC analysis Steady-state response when frequency is varied

## Slide 44: Example of test bench (L=0.15μm)
inv_dc.sch

## Slide 45: Simulation results
Input A=0V vs. Output Y=1.8V
Input A=1.8V vs. Output Y=0V
→It works as a CMOS inverter!

## Slide 46: What is the performance of logic gate, CMOS inverter?
Topology has been determined but the size of CMOS have not yet been determined. → How to determine?
Performance of logic gate
  Drivability (output current）
  fan-out (F.O.)
  delay time（rise delay / fall delay）

## Slide 47: Fanout: Inverter/buffer delay
Thinking about fan-out
  Load of input stage buffer:
  Load of output stage buffer is 10 times of input load
  Place a buffer (2 inverters x 2) in the middle. Consider the fan-out of this buffer.
  Aim to minimize the delay time from ina to outy.
Find the delay time between ina to outy

## Slide 48: Delay time of buffer
Simulate the 6-stage inverter chain Do the transient analysis because we want to see the time vs. voltage waveforms.
Format of transient analysis
tran [time step] [analysis time]

## Slide 49: Example of testbench (L=0.15μm)
How do you determine the fan-out here?
6inv_test.sch

## Slide 50: Example of testbench (L=0.15μm)
1→1→2→5→10→10
1→1→10→10
6inv_test2.sch

## Slide 51: Simulation results
Buffer makes less delay

## Slide 52: Note: fan-out of buffers in standard cells
buf_2 1→2
buf_4 1→4
buf_8 3→8
clkbuf8 2→8
bufbuf8 0.6→1→3→8
buf_12 4→12
buf_16 6→16
clkbuf16 4→16
bufbuf16 1→3→6→16
0.6
3
8
1
If more than 3 - 4 times, insert additional buffer(s)

## Slide 53: What is delay time?
Delay time = (dis)charge time of parasitic capacitance (Input gate capacitance + Output drain capacitance vs. Output current)
In the Elmore delay model, the delay time is calculated by the following approximate formula
Input rise, output fall delay
Input fall, output rise delay
  If do the rise and fall delays match?
  Cdd = drain capacitance on output side Cgg = gate capacitance on input side R = on-resistance on output side
RC time constant of 0.75 and a fixed resistance value

## Slide 54: Cdd, Cgg can be simulated by op analysis
You may find the following formula on the internet MOSFET Input capacitance (Ciss): Ciss = Cgs + Cgd
In LSI CMOS, gate-to-body capacitance must be considered too. Cgg = |Cgs + Cgd + Cgb|
  Gate capacitance is represented by the parameter Cgg
  Output capacitance = Drain capacitance Cdd = |Cdg + Cds + Cdb|
    Cgd and Cdg both represent drain-gate parasitic capacitance. Cdg is the parasitic capacitance that is affected when the drain voltage changes. Cgd is the parasitic capacitance that is affected when the gate voltage changes. Usually, Cdg ≠ Cgd
To find the input / output capacitance, see Cgg / Cdd in op analysis

## Slide 55: Transient response, delay time
Use transient (tran) analysis if you want to find the delay time
To obtain the correct transient response (delay), set the loads on the input and output stages. (load = logic gate; usually, CMOS buffer)
Assuming we design a CMOS inverter with FO=1, we connect buffers of the same size.

## Slide 56: Example of test bench
inv_meas.sch

## Slide 57: Measuring delay time with waveform viewer
Find this output fall delay time

## Slide 58: Measuring delay time with waveform viewer
Input (rise 0.9V) 2.081ns
Output (fall 0.9V) 2.115ns
Difference 33.54ps

## Slide 59: Measuring delay time with commands
Find this output fall delay time
Input: second rise
Output: second fall

## Slide 60: meas command
Calculating delay time from waveforms and graphs is bothersome → meas
This command is multifunctional, but this time we will focus on delay time calculation.
Format of meas command
meas tran [variable] FIND time WHEN [condition] [command]
  [variable] – to assign the result to
  [condition] – “v(net) = Vdd/2”
  [command] – “[RISE / FALL / CROSS] = [number of count]”

## Slide 61: meas command
Calculating delay time from waveforms and graphs is bothersome → meas
This command is multifunctional, but this time we will focus on delay time calculation.
meas command example
meas tran delay1 FIND time WHEN v(vin)=0.9 RISE=2 Assign the time to delay1 when v(vin) is 0.9V at the second rise
meas tran delay2 FIND time WHEN v(vout)=0.9 FALL=2 Assign the time to delay2 when v(vin) is 0.9V at the second fall

## Slide 62: Find the fall delay time with meas command
inv_meas.sch
Input: second rise
Output: second fall

## Slide 63: Find the fall delay time with meas command
Input: second rise
Output: second fall
← Delay time is automatically calculated.
inv_meas.sch

## Slide 64: Also find the rise delay time in the same way
inv_meas.sch

## Slide 65: Rise times and fall times
Fixed to N=1u, changed W of PMOS including buffers of input and output stages
  For N=1u, P=2.1u or 2.2u seems better
Rise and fall delays do not match at
Vth and gm in PMOS and NMOS do not match.
The resistance of the MOSFET (Rds) varies with Vgs.
 | 2.0u | 2.1u | 2.2u | 2.3u
 | 23.238ps | 23.496ps | 23.764ps | 24.035ps
 | 23.889ps | 23.725ps | 23.591ps | 23.482ps
 | 2.0u | 2.1u | 2.2u | 2.3u
 | 23.238ps | 23.496ps | 23.764ps | 24.035ps
 | 23.889ps | 23.725ps | 23.591ps | 23.482ps
（μA）
（V）

## Slide 66: Corner of model
  ss – Model for slow responsiveness (slow-slow)
  tt – Model for typical responsiveness (typical-typical)
Vth of NMOS
Vth of PMOS
ff
fs
sf
ss
tt
High Vth causes Slow response
Low Vth causes Fast response

## Slide 67: Switch of model corner
Just change “tt” to “ss”, “ff”, etc…

## Slide 68: Rise times and fall times
Simulation with different corner model (ss) changes the results.
  For N=1u, P=2.5u or 2.6u seems better.
Rise and fall delays do not match at (On-resistance ratio is P:N = 3:1 in ss) The resistance of the MOSFET varies with Vgs.
 | 2.4u | 2.5u | 2.6u | 2.7u
 | 33.242ps | 33.538ps | 33.856ps | 34.191ps
 | 33.845ps | 33.754ps | 33.724ps | 33.750ps
 | 2.4u | 2.5u | 2.6u | 2.7u
 | 33.242ps | 33.538ps | 33.856ps | 34.191ps
 | 33.845ps | 33.754ps | 33.724ps | 33.750ps

## Slide 69: Background knowledge of LSI
Layout

## Slide 70: Design flow of Analog LSI
Draw schematics and test benches
Simulation
Draw layouts based on schematics
Layout verification
Post-layout simulation: Simulation with parasitic components
（Place on frame）

## Slide 71: Planar MOSFET transistor
Substrate is stacked as the bottom layer.
MOSFET on substrate (well, diffusion, poly)
Wiring above the transistor(metal*, via*)
MIMCAP can be made by sandwiching an insulator between metals (metal3-capm and metal4-cap2m)

## Slide 72: MIMCAP
2 MIMCAPs exist between M5-M4 and M4-M3
Crossed wiring layers also make a capacitor, but small capacitance. (so-called MOMCAP) →Cause of parasitic capacitance
Capacitor Consisting only of Metal1 and Metal2

## Slide 73: Double well, Twin well, Dual well
CMOS transistors are composed of N-well and P-substrate Pcell generates double-well CMOS by default.
https://note.com/akira_tsuchiya/n/n416b7f74b701
PMOS has an individual well so body voltage is variable
Body of all double well NMOS are connected via substrate
(Lowest voltage in the LSI chip, GND, VSS)

## Slide 74: Triple well
CMOS transistors are composed of Deep N-well, P-well and N-well The cross section described in the PDK documents is triple well.
NMOS has an individual well so body voltage is variable
Example of applications
・Adjust Vth (body effect)
・Cascode connection with body connected to source
・Block noise from substrate
etc…
https://note.com/akira_tsuchiya/n/nd4444304f013
PMOS
NMOS

## Slide 75: Body effect
Bias voltage applied to the body changes transistor characteristics.
Threshold voltage（Vth）varies
  Drain-source current (Ids) varies (when compared with fixed gate voltage)

## Slide 76: nMOS diagram
D
G
n+
p
n+
S
B

## Slide 77: nMOS diagram
n
D
G
S = GND
n+
B=GND
n
p
n
n+
no current yet
Since Vd > Vs,
the depletion layer on the drain side is larger than the depletion layer on the source side
Hole on substrate moves to gate at Vg > 0
→formation of deplation layer

## Slide 78: nMOS diagram
D
G >> 0V
S = 0V
n
B = 0V
p
have a current
n+
n+
Inversion layer is easily formed when the depletion layer is thin and difficult to form when it is thick
Conduction electrons become majority carriers at Vg >> 0
→Formation of inversion layer (Vth)

## Slide 79: nMOS diagram
D
S = 0V
B < 0V
p
hard to conduct
n+
When Vb < 0, the depletion layer spreads
→ Inversion layer becomes harder to form (Vth increases) and thinner (on-resistance increases)
n+
G >> 0V
Inversion layer is easily formed when the depletion layer is thin and difficult to form when it is thick
Conduction electrons become majority carriers at Vg >> 0
→Formation of inversion layer (Vth)

## Slide 80: nMOS diagram
D
S = 0V
B > 0V
p
easy to conduct
n+
n+
When Vb > 0, the depletion layer narrows
→ Inversion layer becomes easier to form (Vth decreases) and thicker (on-resistance decreases)
G >> 0V
Inversion layer is easily formed when the depletion layer is thin and difficult to form when it is thick
Conduction electrons become majority carriers at Vg >> 0
→Formation of inversion layer (Vth)

## Slide 81: Body effect in nMOS
trbench_body.sch

## Slide 82: nMOS diagram
G
p
Inversion layer is easily formed when the depletion layer is thin and difficult to form when it is thick
Conduction electrons become majority carriers at Vg >> 0
→Formation of inversion layer (Vth)
n+
n+
B >> 0V
D
S = GND
Current conducts from B to S

## Slide 83: nMOS diagram
G
S = GND
p
Conduction electrons become majority carriers at Vg >> 0
→Formation of inversion layer (Vth)
n+
n+
B = 1.8V
D=1.8V
If drain and body are shorted, it will not function as a transistor.
Inversion layer is easily formed when the depletion layer is thin and difficult to form when it is thick

## Slide 84: Body effect in nMOS
Vth of body diode
Vth of body diode
trbench_body.sch

## Slide 85: To apply bias voltage to the body
Since the transistor will conduct and fail if the biasing of body diode exceeds , Bias voltage is applied as long as it does not exceed that value.
Triple well is required to bias body in nMOS.
  More complicated to draw and larger area than double well.
  Triple-well is disadvantageous in logic circuits. The larger the area, the lower the density.
Double well is recommended if there is no preference since it is disadvantageous in terms of integration density.
Connect the body of PMOS to VDD and the body of NMOS to GND (VSS, ±0V)

## Slide 86: Example: 2-input NAND
M6_B ≠ M8_B = GND M6 must be triple well
M2_B = M4_B = GND M2 can be double well

## Slide 87: Planar Pch MOSFET transistor（triple well）
Polysilicon
Deep N-well
N-well
P+
Oxide insulating layer
Pshophorus-Silicate Glass; Insulators to fill in between layers
P-substrate
Shallow Trench Isolation
STI avoids leakage current
・Improve withstand voltage
・Avoid latch-up (occurs in PNPN)

## Slide 88: Planar Pch MOSFET transistor
poly
diff (diffusion)
psdm (n+)
nwell N-well
diff / active Diffusion layer of different polarity from well or substrate
psdm P+ implant
poly Polysilicon
dnwell is not drawn by default. (not necessary even for triple well)
nwell

## Slide 89: Planar Nch MOSFET transistor（triple well）
Polysilicon
P-well
Shallow Trench Isolation
N+
Pshophorus-Silicate Glass; Insulators to fill in between layers
Deep N-well
P-substrate
Oxide insulating layer
STI avoids leakage current
・Improve withstand voltage
・Avoid latch-up (occurs in PNPN)

## Slide 90: Planar Nch MOSFET transistor
poly
diff (diffusion)
nsdm (n+)
diff / active Diffusion layer of different polarity from well or substrate
nsdm N+ implant
poly Polysilicon
pwell and dnwell are not drawn by default.

## Slide 91: Planar Nch MOSFET transistor
Poly-Oxide-Diff sandwich is the M-O-S transistor.
The direction of L and W is determined by the direction of current

## Slide 92: Poly resistor
The direction of L and W is determined by the direction of current
W/L of poly resistor is opposite to MOSFET

## Slide 93: Planar MOSFET transistor（Triple well）
p-substrate
Well of each transistor is a body in the triple-well.
The P-well of nMOS is isolated from the P-substrate by the Deep N-well.
Gate
Gate
High voltage side is Source, low voltage side is Drain in pMOS
High voltage side is Drain, low voltage side is Source in nMOS
Deep N-well

## Slide 94: Body connection: tap
Default PFET and NFET are 3-terminal devices and have no body terminals.
Use TAP layer to connect to the body.

## Slide 95: Body connection: tap
Default PFET and NFET are 3-terminal devices and have no body terminals.
Use TAP layer to connect to the body.
* = Drain or Source
G
G
G
G
*
*
*
*
*
*
*
*
B
B

## Slide 96: Body connection in Pcell
PFET is connected to N-well via N+. NFET is connected to P-substrate via P+. + indicates a high doping concentration, which has the effect of reducing contact resistance
https://note.com/akira_tsuchiya/n/nd4444304f013

## Slide 97: Layer names and meanings
nwell N-well
diff Diffusion layer of different polarity from well or substrate
tap Diffusion layer of the same polarity as the well or substrate
psdm P+ implant
nsdm N+ implant
poly Polysilicon
licon1 Contact (Via) to li1 (metal layer)
npc Nitride Poly Cut (polysilicon exposed area)
li1 local interconnect (metal layer)

## Slide 98: Layer names and meanings
The top of polysilicon is insulated with nitride (not PSG). npc is a nitride masking layer.
When connecting licon1 (contact to li1), it is necessary to draw npc as well.

## Slide 99: Layer names and meanings

## Slide 100: Layer to pass LVS check in tapless design: well.pin
When designing the layout without taps (contacts to body), well.pin can avoid body connection violations in LVS.
well.pin specifies the net name of the substrate / well. Don’t forget that you need to connect the body with tap cells.
nwell.pin
pwell.pin (even with p-substrate)

## Slide 101: Layout
Layout: Planar FET

## Slide 102: How to draw the layout
１．Make a LVS schematic (Xschem) ・ Delete non-schematic symbols such as power source (idc, vdc...) and commands ・ Replace Global net symbol (vdd, gnd...) with iopin.sym
２．Draw the layout ・ You should run DRC every couple of operations until you get used to it.
３．DRC(Design Rules Check) ・ If you don’t pass DRC, foundries will not make a chip.
４．LVS (Layout Versus Schematic) ・ Compare your layout with the LVS schematic and check if it is drawn correctly.
５．PEX (Parasitic Extraction)
Layout
verification

## Slide 103: Example layouts of CMOS inverter (NOT logic gate)

## Slide 104: Notes
Do not violate design rules https://skywater-pdk.readthedocs.io/en/main/rules/periphery.html
  Run Klayout DRC (Caravel) to verify that there are no errors and no violations.
  Run Klayout LVS to verify that your layout is equal to the LVS schematic.
    If they do not match, post-layout simulation will not work properly. Of course, real chip may not work too.
    Magic DRC/LVS is also available.

## Slide 105: 2-input NAND layout based on Pcell

## Slide 106: Major design rules
SKY130

## Slide 107: Design rules
All design rules are here
  https://skywater-pdk.readthedocs.io/en/main/rules/periphery.html
Here are some important design rules for drawing CMOS inverters
Transistors are automatically generated by Pcell, so we will focus on the metal layer.

## Slide 108: GRID / OFFGRID
x.1b: All layers must be on a grid of 0.005μm.
  Some layers (met1, via, met2) are available down to 0.001μm (x.1a),
  however, the Klayout DRC is unified at 0.005μm for all layers.
  For example, when you draw the rectangle, the coordinates of 4 points must be 0.005μm steps.
OFFGRID error occurs when the coordinate finer than 0.005μm is specified

## Slide 109: npc.drawing : Nitride Poly Cut
npc.1 : Minimum width : 0.270 μm
npc.2 : Minimum space of npc to npc: 0.270 μm
npc.4 : Minimum space of npc to diff/tap: 0.090 μm

## Slide 110: licon1.drawing : Local Interconnect Contact
licon.1 : Contact size must be 0.170 μm×0.170 μm licon.2 : Minimum space of licon to licon: 0.170 μm
Minimum enclosure of licon by diff: licon.5a : In either one of the x,y axes : 0.040 μm licon.5c : In the other of the x,y axes : 0.060 μm
Minimum enclosure of licon by tap: licon.7 : In either one of the x,y axes : 0.120 μm licon.6 : May contact in the other axis, but must not overhang licon.5b : Min space between tap_licon and diff-abutting tap edge: 0.060μm from diff
Minimum enclosure of licon by poly: licon.8 : In either one of the x,y axes : 0.050 μm licon.8a : In the other of the x,y axes : 0.080 μm

## Slide 111: li1.drawing : Local Interconnect
li.1 : Minimum space : 0.170 μm li.2 : Maximum L/W ratio without licon or mcon : 10 DRC cannot check li.2 rule li.3 : Minimum space of li to li : 0.170μm li.6 : Minimum area : 0.0561 μ
Minimum enclosure of li1 by licon: li.5 : In either one of the x,y axes : 0.080 μm licon.6 :May contact in the other axis, but must not overhang

## Slide 112: mcon.drawing : Metal Contact (li1 - met1)
ct.1 : Contact size must be 0.170 μm×0.170 μm ct.2 : Minimum space of mcon to mcon : 0.190 μm
Minimum enclosure of mcon by li: ct.4 : mcon must not overhang li1.drawing (0.000 μm)
Minimum enclosure of met1 by mcon: m1.4 : In either one of the x,y axes : 0.030 μm m1.5 : In the other of the x,y axes : 0.060 μm

## Slide 113: met1/2/3.drawing : Metal
met1.drawing : m1.1 : Minimum width : 0.140 μm m1.2 : Minimum space of met1 to met1: 0.140 μm m1.6 : Minimum area : 0.083 μ
met2.drawing : m2.1 : Minimum width : 0.140 μm m2.2 : Minimum space of met2 to met2 : 0.140 μm m2.6 : Minimum area : 0.0676 μ
met3.drawing : m3.1 : Minimum width : 0.300 μm m3.2 : Minimum space of met3 to met3 : 0.300 μm m3.6 : Minimum area : 0.240 μ

## Slide 114: via.drawing : Via (met1 - met2)
via.1 : Contact size must be 0.150 μm×0.150 μm via.2 : Minimum space of via to via : 0.170 μm
Minimum enclosure of via by met1: via.4 : In either one of the x,y axes : 0.055 μm via.5 : In the other of the x,y axes : 0.085 μm
Minimum enclosure of met2 by via: m2.4 : In either one of the x,y axes : 0.055 μm m2.5 : In the other of the x,y axes : 0.085 μm

## Slide 115: via2.drawing : Via2 (met2 – met3)
via.1 : Contact size must be 0.200 μm×0.200 μm via.2 : Minimum space of via to via : 0.200 μm
Minimum enclosure of via2 by met2: via.4 : In either one of the x,y axes : 0.040 μm via.5 : In the other of the x,y axes : 0.085 μm
Minimum enclosure of met3 by via2: m3.4 : 0.065 μm on all four sides.

## Slide 116: Post-layout simulation
Parasitic extraction

## Slide 117: Layout Validation: PEX, Parasitic Extraction
RC extraction Make a netlist with parasitic resistance and parasitic capacitance
C extraction Make a netlist with parasitic capacitance only

## Slide 118: Preparation before PEX: Flatten
1. Save the copy of your layout
  Using UPPERCASE LETTERS in file name may cause some bugs.
    Change the extension from .GDS to .gds
2. Run Cells > Flatten Cell > All hierarchy levels
3. Make sure that “Cells” is TOP (or the name you set) only and save it.

## Slide 119: Parasitic extraction
Run the parasitic capacitance extraction using Magic PEX.
  Run Magic PEX (C extraction)
A netlist with parasitic capacitance is generated
Filename：{layout name}_pex_extracted.spice
    Default: TOP_pex_extracted.spice

## Slide 120: Example of a delay time simulation
CMOS inverter
  The size of first stage is
  Output load capacitance is the same as input:
  Simulate the delay time from ina to outy

## Slide 121: Example of a test bench for measuring ideal delay time

## Slide 122: Modify the test bench to post-layout simulation
The following changes are required for post-layout simulation
PATH to the extracted netlist
Symbol for the extracted netlist

## Slide 123: Set the PATH to the extracted netlist
・Set the PATH to the extracted netlist by .include ・ Extracted netlist is in the same directory as the layout (.gds)

## Slide 124: How to make a symbol for the extracted netlist
Make a symbol from LVS schematic
  Menu Symbol > Make symbol from schematic
Generated symbol refer to the LVS schematic. We have to modify this to refer to the extracted netlist.

## Slide 125: How to make a symbol for the extracted netlist
Open the symbol's property and set like this (key binding: Q)
type=primitive format=“@name [pins in netlist] @prefix“ template=“name=x1 prefix=[title of subckt]“ extra=“prefix“ highlight=true
See http://repo.hu/projects/xschem/xschem_man/symbol_property_syntax.html

## Slide 126: How to make a symbol for the extracted netlist
Example of CMOS inverter
type=primitive format="@name @@A @@Y @@VDD @@GND @prefix“ template="name=x1 prefix=TOP“ extra="prefix“ highlight=true
Describe in the same order as the pins in the extracted netlist

## Slide 127: How to make a symbol for the extracted netlist
Example of CMOS inverter
type=primitive format="@name @@A @@Y @@VDD @@GND @prefix“ template="name=x1 prefix=TOP“ extra="prefix“ highlight=true
Add “@@” prefix to the pins.
Now the symbol works.

## Slide 128: How to make a symbol for the extracted netlist (2)
Open the symbol's property and set like this (key binding: Q)
type=primitive format=“@name [pins in netlist] @prefix“ template=“name=x1 [Pins to specify net in property] prefix=[title of subckt]“ extra=“ [Pins to specify net in property] prefix“ highlight=true
See http://repo.hu/projects/xschem/xschem_man/symbol_property_syntax.html

## Slide 129: How to make a symbol for the extracted netlist (2)
Remove VDD and GND pins from the symbol and describe them in the property
type=primitive format="@name @@A @@Y @VDD @GND @prefix“ template="name=x1 VDD=VDD GND=0 prefix=TOP“ extra=“VDD GND prefix“ highlight=true
To specify a net of pin in the property, add “@” prefix in format,
add pins in extra and add default valueds in template.

## Slide 130: How to make a symbol for the extracted netlist (2)
Remove VDD and GND pins from the symbol and describe them in the property
type=primitive format="@name @@A @@Y @VDD @GND @prefix“ template="name=x1 VDD=VDD GND=0 prefix=TOP“ extra=“VDD GND prefix“ highlight=true
easier to see!
VDD=VDD
GND=0
inv.sym

## Slide 131: Test bench modification (before)

## Slide 132: Test bench modification (after)
inv_pex.sch

## Slide 133: Simulation results
149.9ps
15.0ps
164.9ps
Parasitic capacitance worsens responsiveness
After
Before

## Slide 134: Tips

## Slide 135: Tips
Multi finger and Mismatch simulation
Monte Carlo simulation
Analog switch and Pass Transistor Logic
D latch and D flip-flop

## Slide 136: Multi finger
Layout Techniques

## Slide 137: FO of buffers in standard cells
buf_2 1→2
buf_4 1→4
buf_8 3→8
clkbuf8 2→8
bufbuf8 0.6→1→3→8
buf_12 4→12
buf_16 6→16
clkbuf16 4→16
bufbuf16 1→3→6→16
0.6
3
8
1

## Slide 138: 3 stage inverter
Two transistors with the same node and the same size equals a transistor with twice W

## Slide 139: 3 stage inverter
6.6 / 3 divided into (1.65 / 0.75) *4
  (6.6/3) *3 -> (1.65 / 0.75) *12
  Flatten before edit
LVS will pass without schematic modification.

## Slide 140: Mismatch simulation
Multi-finger has the effect of reducing mismatch (variation between elements)
Mismatch simulations are available to look at element-to-element variation.
Assign a random Vth to each element
Append _mm to the end of the corner such as “tt_mm”

## Slide 141: Test bench example
mm_sim.sch

## Slide 142: Variation in 30 runs with the same seed
Both LVS schematics are identical.
inv12.gds, inv12.sym
inv3.gds, inv3.sym

## Slide 143: Monte Carlo simulation
Simulation by random characteristics

## Slide 144: Monte Carlo simulation
  Usually, we specify the corner of model in the testbench.
  Monte Carlo simulation runs multiple simulations with random characteristics
  In SKY130, “mc” corner is a Monte Carlo method model.
Vth of NMOS
Vth of PMOS
ff
fs
sf
ss
tt
High Vth causes Slow response
Low Vth causes Fast response

## Slide 145: Xschem testbench (mc, 10 times, L=0.15μm)
test_inv_mc.sch

## Slide 146: Simulation results (mc)

## Slide 147: Pass transistor logic
Transmission gate, Analog switch

## Slide 148: 2-input AND
A | B | Q
L | L | L
L | H | L
H | L | L
H | H | H

## Slide 149: 2-input AND as one-way switch
B | A | Q
L | L or H | L
H | L | L
H | H | H
A | B | Q
L | L or H | L
H | L | L
H | H | H
When OFF, the switch is in a circuit-breaking state in the real switch, but in the AND gate, it is connected to GND.

## Slide 150: 2-input NAND
Inverted output of 2-input AND
A | B | Q
L | L | H
L | H | H
H | L | H
H | H | L
Inverted NAND is treated as AND in CMOS circuits.

## Slide 151: Analog switch (transmission gate + inverter)
φ | A | Q
L | High resistance (Hi-Z) | Hi-Z
H | Almost conduction (PASS) | 
On-resistance (Rds)

## Slide 152: 2-input AND (left) vs. analog switch (right)
B | A | Q
L | L or H | L
H | L | L
H | H | H
φ | A | Q
L | Hi-Z | Hi-Z
H | PASS | L
In analog switches, when φ = Low, the output is almost insulated (high resistance, Hi-Z)
In AND gate, when B=Low, it is connected to GND (Low)

## Slide 153: 2-input XOR
Logic circuits prohibit short-circuiting of outputs. XOR design with logic circuits is a bit complicated. (NOR (4) + AOI (6) = 10 transistors)
https://www.pngwing.com/en/free-png-iloox

## Slide 154: 2-input XOR
Analog switch is Hi-Z at φ=Low, that is, output can be shorted if controlled carefully. Number of transistors may be reduced.
Unintentional Hi-Z (floating) input is undesirable. The logic output must be always High or Low.
https://en.wikipedia.org/wiki/XOR_gate

## Slide 155: Simulation of the analog switch

## Slide 156: Simulation of the analog switch
Output of analog switch is Hi-Z
= Input of buffer is floating

## Slide 157: D latch and D flip-flop
Logic gates with floating gates

## Slide 158: Floating gate
The drain-source current (Ids) is determined by the gate-source voltage (Vgs), but the gate has a parasitic capacitance.
When the gate is in the floating state, the gate holds the gate-source voltage (Vgs) that was input immediately before.
It is called a floating gate and is used in the D latch, D flip-flop and SRAM.

## Slide 159: Gated D flip-flop / D latch
Holds the value of D when E goes from High to Low
When E=High, the state of D is reflected in Q (PASS)
E is sometimes expressed as CLK.
E (CLK) | D | Q
L | X | Hold
H | L | L
H | H | H

## Slide 160: Gated D flip-flop / D latch
Gated D flip-flop / D latch using transmission gates
Some logic ICs are using transmission gates (TG) to make a D latch
CD4042B
CD74HC75
↓Need an inverter to invert E (=XE)

## Slide 161: Gated D flip-flop / D latch
Left: TC4042B Right: TC74HC75
Clocked Inverter

## Slide 162: Example of D latch with clocked inverter

## Slide 163: Example of D latch with clocked inverter

## Slide 164: Waveform example of logical operation check
dlatch_bench2.sch

## Slide 165: Positive-edge-triggered D flip-flop / D flip-flop
In a D latch, when CLK(E) was High, output Q was a pass.
In D flip-flop, output Q changed only when CLK goes from Low to High
CLK | D | Q
L→H | L | L
L→H | H | H
otherwise | X | hold

## Slide 166: Positive-edge-triggered D flip-flop / D flip-flop
It can be made with two D latches. (so-called Master-slave edge-triggered D flip-flop)
Logic ICs often use two D latches to make a D flip-flop
Negative-edge-triggered D flip-flop

## Slide 167: Positive-edge-triggered D flip-flop / D flip-flop
Left: CD4013B Right: CD74HC74

## Slide 168: Positive-edge-triggered D flip-flop / D flip-flop
Left: TC4013BP Right:TC74HC74

## Slide 169: Example of a D flip-flop with two D latches

## Slide 170: Example of a D flip-flop with two D latches

## Slide 171: f/2, f/4, f/8 Clock divider
fdiv.sch

## Slide 172: f/2, f/4, f/8 Clock divider

## Slide 173: 3-bit Shift register
shift.sch

## Slide 174: 3-bit Shift register

## Slide 175: 3-bit Johnson ring counter
johnson.sch

## Slide 176: 3-bit Johnson ring counter